## Experiment Title: Development of a Novel Catalytic System for Cross-Coupling Reactions

**Date:** March 15, 2025

**Researcher:** Len

**Lab/Project:** Catalysis and Sustainable Chemistry

**Objective:**

To develop and characterize a palladium-free catalytic system for Suzuki-Miyaura cross-coupling reactions using iron-based nanoparticles.

**Materials & Reagents:**

1. Catalytic Materials:

· Iron(III) chloride hexahydrate

· Sodium borohydride

· Polyvinylpyrrolidone (PVP, stabilizer)

· Graphene oxide (support material)

2. Reaction Components:

· 4-Bromoacetophenone

· Phenylboronic acid

· Potassium carbonate (base)

· Tetrahydrofuran (solvent)

3. Equipment:

· Schlenk line

· Rotary evaporator

· GC-MS system

· TEM microscope

· Glovebox (nitrogen atmosphere)

**Procedure:**

1. Synthesize Fe nanoparticles by reducing FeCl₃·6H₂O with NaBH₄ in the presence of PVP under N₂.

2. Deposit nanoparticles onto graphene oxide support via sonication for 30 minutes.

3. Characterize catalyst using TEM and XPS.

4. Set up cross-coupling reaction: 4-bromoacetophenone (1 mmol), phenylboronic acid (1.2 mmol), K₂CO₃ (2 mmol), and Fe catalyst (5 mol%) in THF.

5. Heat reaction at 80°C for 12 hours under nitrogen.

6. Monitor conversion by GC-MS and isolate product via column chromatography.

**Results & Observations:**

· TEM showed uniform Fe nanoparticles (15 ± 3 nm) on graphene oxide.

· Cross-coupling yield: 78% with >95% selectivity for the desired product.

· Catalyst showed good recyclability (75% activity after 3 cycles).

· Control experiment without catalyst showed no product formation.

**Conclusion & Next Steps:**

· Successfully developed an alternative to traditional Pd catalysts with good activity.

· Next experiments will focus on expanding substrate scope and optimizing reaction conditions.

· Plan to investigate catalyst leaching and long-term stability.