## Experiment Title: Electrochemical CO₂ Reduction Using Novel Cu-Based Catalysts

**Date:** April 3, 2025

**Researcher:** Len

**Lab/Project:** Renewable Energy Materials

**Objective:**

To evaluate the electrocatalytic activity of copper-zinc oxide nanocomposites for CO₂ reduction to value-added products.

**Materials & Reagents:**

1. Catalyst Preparation:

· Copper(II) nitrate trihydrate

· Zinc nitrate hexahydrate

· Sodium citrate (chelating agent)

· Sodium hydroxide (precipitating agent)

2. Electrochemical Setup:

· Nafion solution (5 wt%)

· Carbon paper (electrode substrate)

· KHCO₃ electrolyte solution (0.1 M)

· CO₂ gas (99.999% purity)

3. Equipment:

· Potentiostat/galvanostat

· H-cell electrochemical cell

· Gas chromatography system

· SEM microscope

· XRD instrument

**Procedure:**

1. Prepare Cu-ZnO nanocomposites via co-precipitation method at controlled pH (9.5).

2. Anneal catalyst at 350°C for 3 hours under 5% H₂/N₂ atmosphere.

3. Prepare catalyst ink by dispersing 5 mg of catalyst in ethanol with 20 μL Nafion.

4. Deposit ink on carbon paper (1 cm²) and dry at room temperature.

5. Assemble H-cell with Ag/AgCl reference electrode and Pt counter electrode.

6. Purge electrolyte with CO₂ for 30 minutes before measurements.

7. Perform linear sweep voltammetry (LSV) from 0 to -1.2 V vs. RHE.

8. Conduct chronoamperometry at -0.8 V for 2 hours, collecting gas products for GC analysis.

**Results & Observations:**

· XRD confirmed the formation of Cu-ZnO nanocomposites with average crystallite size of 12 nm.

· SEM showed uniform particle distribution across the carbon substrate.

· Faradaic efficiency: 42% for CO, 35% for formate, and 10% for methanol at -0.8 V vs. RHE.

· Current density stabilized at 15 mA/cm² after initial decrease.

**Conclusion & Next Steps:**

· The Cu-ZnO catalyst shows promising activity for CO₂ reduction with good selectivity.

· Further optimization required to improve methanol selectivity.

· Plan to investigate the effect of Cu:Zn ratio on product distribution.