## Experiment Title: Synthesis and Characterization of Photoresponsive Liquid Crystals

**Date:** May 12, 2025

**Researcher:** Len

**Lab/Project:** Smart Materials Development

**Objective:**

To synthesize azobenzene-containing liquid crystal compounds and characterize their photoresponsive properties for potential applications in smart displays.

**Materials & Reagents:**

1. Synthesis Components:

· 4-Hydroxyazobenzene

· 4'-Bromo-4-biphenylcarboxaldehyde

· Potassium hydroxide

· Dimethylformamide (DMF)

· Anhydrous magnesium sulfate

2. Characterization Materials:

· Polarized optical microscopy slides

· Differential scanning calorimetry (DSC) pans

· UV light source (365 nm)

· Visible light source (450 nm)

3. Equipment:

· Reflux setup

· Polarized optical microscope (POM)

· UV-Vis spectrophotometer

· DSC analyzer

· FTIR spectrometer

**Procedure:**

1. Dissolve 4-hydroxyazobenzene (1 eq) and KOH (1.2 eq) in DMF and stir for 30 minutes.

2. Add 4'-bromo-4-biphenylcarboxaldehyde (1 eq) and heat at 80°C for 8 hours.

3. Cool, pour into water, filter precipitate, and recrystallize from ethanol.

4. Confirm structure by ¹H-NMR, ¹³C-NMR, and FTIR spectroscopy.

5. Determine phase transitions using DSC (heating/cooling rate: 10°C/min).

6. Analyze liquid crystal textures using POM at different temperatures.

7. Measure UV-Vis spectra before and after UV irradiation (365 nm, 5 min).

**Results & Observations:**

· FTIR confirmed successful formation of ether linkage (C-O-C stretch at 1245 cm⁻¹).

· DSC showed clear phase transitions: crystal → smectic A (85°C) → nematic (95°C) → isotropic (115°C).

· POM revealed characteristic schlieren texture for nematic phase.

· UV irradiation caused trans→cis isomerization, confirmed by decrease in absorption at 350 nm and increase at 450 nm.

· Phase transition temperatures decreased by ~8°C after UV exposure due to molecular conformational changes.

**Conclusion & Next Steps:**

· Successfully synthesized photoresponsive liquid crystal with reversible photoswitching properties.

· Next experiments will focus on incorporating this compound into polymer matrices.

· Plan to study the kinetics of thermal relaxation of the cis isomer.