## Experiment Title: Green Synthesis of Silver Nanoparticles Using Plant Extracts

**Date:** June 8, 2025

**Researcher:** Len

**Lab/Project:** Nanomaterials for Antimicrobial Applications

**Objective:**

To develop an environmentally friendly method for synthesizing silver nanoparticles using aqueous extracts of Camellia sinensis (green tea) and evaluate their antimicrobial properties.

**Materials & Reagents:**

1. Synthesis Materials:

· Silver nitrate (AgNO₃, 1 mM solution)

· Dried green tea leaves

· Deionized water

· pH adjustment buffers

2. Characterization Materials:

· UV-vis cuvettes

· TEM grids

· Mueller-Hinton agar

· Bacterial cultures (E. coli, S. aureus)

3. Equipment:

· UV-Vis spectrophotometer

· TEM microscope

· DLS particle analyzer

· Incubator (37°C)

· Zone of inhibition measurement tool

**Procedure:**

1. Prepare green tea extract: boil 5 g dried leaves in 100 mL deionized water for 5 minutes, filter, and cool.

2. Mix 10 mL of extract with 90 mL of AgNO₃ solution (1 mM) and stir at room temperature.

3. Monitor color change from pale yellow to brown/dark brown, indicating nanoparticle formation.

4. Characterize nanoparticles using UV-Vis spectroscopy (surface plasmon resonance peak).

5. Analyze size and morphology using TEM and DLS.

6. Test antimicrobial activity using agar well diffusion method against E. coli and S. aureus.

7. Measure zones of inhibition after 24-hour incubation at 37°C.

**Results & Observations:**

· Color change observed within 30 minutes, indicating rapid reduction of Ag⁺ to Ag⁰.

· UV-Vis spectrum showed characteristic surface plasmon resonance peak at 425 nm.

· TEM revealed spherical nanoparticles with average size of 18 ± 4 nm.

· Zeta potential of -32.5 mV indicated good colloidal stability.

· Antimicrobial testing showed zones of inhibition: 12 mm for E. coli and 14 mm for S. aureus.

**Conclusion & Next Steps:**

· Successfully synthesized stable silver nanoparticles using green tea extract as both reducing and capping agent.

· The nanoparticles demonstrated good antimicrobial activity against both Gram-positive and Gram-negative bacteria.

· Next experiments will investigate the effects of reaction parameters (temperature, pH, extract concentration) on nanoparticle characteristics.

· Plan to evaluate cytotoxicity against mammalian cell lines.