## Experiment Title: Development of pH-Responsive Hydrogels for Controlled Drug Release

**Date:** July 20, 2025

**Researcher:** Len

**Lab/Project:** Advanced Drug Delivery Systems

**Objective:**

To synthesize and characterize poly(acrylic acid-co-acrylamide) hydrogels with pH-responsive properties for controlled release of model drug compounds.

**Materials & Reagents:**

1. Synthesis Components:

· Acrylic acid (AA)

· Acrylamide (AAm)

· N,N'-methylenebisacrylamide (MBA, crosslinker)

· Ammonium persulfate (APS, initiator)

· N,N,N',N'-tetramethylethylenediamine (TEMED, catalyst)

2. Characterization Materials:

· Methylene blue (model drug)

· Buffer solutions (pH 2.0, 5.0, 7.4)

· Deionized water

· Dialysis membrane (MWCO 12-14 kDa)

3. Equipment:

· Reaction vessel with nitrogen inlet

· Rheometer

· UV-Vis spectrophotometer

· FTIR spectrometer

· SEM microscope

**Procedure:**

1. Prepare monomer solution: mix AA (70 mol%) and AAm (30 mol%) in deionized water.

2. Add MBA crosslinker (1 mol% of total monomer).

3. Degas solution with nitrogen for 15 minutes.

4. Add APS (1 wt%) and TEMED (0.5 wt%) to initiate polymerization.

5. Cast solution into molds and allow polymerization for 24 hours at room temperature.

6. Wash hydrogels with deionized water for 3 days, changing water daily.

7. Freeze-dry samples for characterization.

8. Test swelling behavior at different pH values (2.0, 5.0, 7.4).

9. Load methylene blue by soaking hydrogels in 0.1% solution for 24 hours.

10. Study drug release profiles in different pH buffers using UV-Vis spectroscopy.

**Results & Observations:**

· FTIR confirmed successful copolymerization (C=O stretch at 1720 cm⁻¹ for AA, amide bands at 1655 and 1610 cm⁻¹ for AAm).

· SEM showed porous structure with interconnected networks.

· Swelling ratio at pH 7.4 (452%) was significantly higher than at pH 2.0 (87%) due to ionization of carboxyl groups.

· Drug release kinetics: 25% release at pH 2.0 vs. 85% release at pH 7.4 after 24 hours.

· Release data fitted well with Korsmeyer-Peppas model (n = 0.58), indicating anomalous transport mechanism.

**Conclusion & Next Steps:**

· Successfully synthesized pH-responsive hydrogels with significantly different swelling and release properties in acidic vs. neutral conditions.

· The system shows potential for targeted delivery to intestinal environments (pH ~7) versus gastric environments (pH ~2).

· Next steps include optimizing AA:AAm ratio for specific release profiles and testing with actual therapeutic compounds.

· Plan to investigate temperature-responsive components for dual-responsive systems.